GUIDE SPECIFICATION

SECTION 03360

CONCRETE FINISHES

DRY-SHAKE COLORED HARDENER 
[STAMPED/IMPRINTED CONCRETE PAVEMENT]

******************************************************************************

This guide specification is intended to be used by a qualified construction specifier.  It is not intended to be used verbatim as a project specification without appropriate modifications for the specific use intended.

Notes for review by the specifier are set off from specification text by rows of asterisks.  Optional text requiring a selection is enclosed within brackets, e.g., "Color shall be [gray] [white]."  Items requiring input specifier input are enclosed within brackets, e.g., "Color: [_______]."

******************************************************************************

- GENERAL

  - SUMMARY

    - Drawings and general provisions of Contract, including General and Supplementary Conditions and Division 1 Specification sections, apply to Work of this Section.

    - Section Includes:

      - Dry-shake colored hardener applied to [slabs-on-grade,] [sidewalks,] [driveways,] [patios,] [roads,] [parking lots,] [_______,] [and] [other exterior concrete pavements].

      - [Stamping/Imprinting.]

      - Curing of colored [and imprinted] concrete.

    - Related Sections:

      - Division 3 Section "Cast-In-Place Concrete for general applications of concrete [and for cementitious or epoxy mortar, underlayments, or toppings].

      - Division 7 Section "Joint Sealants" for colored sealants for joints.

  - REFERENCES

******************************************************************************

Other useful publications about colored concrete include:

PCA PA124 - Finishing Concrete Slabs with Color and Texture.

PCA SP021 - Color and Texture in Architectural Concrete.

******************************************************************************

    - American Concrete Institute (ACI):

      - ACI 301 "Specification for Structural Concrete for Buildings."

      - ACI 302 IR "Recommended Practice for Concrete Floor and Slab Construction."

      - ACI 303.1 "Standard Specification for Cast-In-Place Architectural Concrete."

      - ACI 304 "Recommended Practice for Measuring, Mixing, Transporting and Placing of Concrete."

      - ACI 305R "Recommended Practice for Hot Weather Concreting."

      - ACI 306R "Recommended Practice for Cold Weather Concreting."

    - American Society of Testing and Materials (ASTM):

      - ASTM C309 "Standard Specifications for Liquid Membrane-Forming Compounds for Curing Concrete."

      - ASTM C494 "Standard Specification for Chemical Admixtures for Concrete."

  - SUBMITTALS

    - Product Data:  Submit manufacturer’s complete technical data sheets for the following:

      - Dry-shake colored hardener.

      - [Powder antiquing release agent] or [Liquid clear release agent.]

      - Imprinting/Texturing tools.

      - Curing compound.

    - Design Mixes:  For each type of concrete.

    - Samples for Initial Selection:  Manufacturer's color charts showing full range of colors available.

    - Qualification Data:  For firms indicated in "Quality Assurance" Article, including list of completed projects.

  - QUALITY ASSURANCE

    - Manufacturer Qualifications:  Manufacturer with 10-years experience in manufacture of specified products.

    - Installer Qualifications: An installer with [5-] [________] years experience with work of similar scope and quality.

    - Comply with the requirements of ACI 301.

    - Obtain each specified material from same source and maintain high degree of consistency in workmanship throughout Project.

    - Notification of manufacturer's authorized representative shall be given at least 1-week before start of Work.

******************************************************************************

Color charts and small sample submittals provide only a general indication of color; color and appearance of completed work may differ.  On large or critical projects, specify a mock-up or field sample to demonstrate that proposed materials and workmanship produce acceptable concrete appearance.

******************************************************************************

    - Colored Concrete [Mockups] [Field Samples]:

      - Provide under provisions of Division 1 Section ["Quality Control."] [________.]

      - At location on Project selected by [Architect] [Landscape Architect] [Engineer], place and finish [10 feet by 10 feet (3 by 3 m)] [4 feet by 4 feet (1.2 by 1.2 m)] [________] area.

      - Construct [mockup][sample panel] using processes and techniques intended for use on permanent work, including curing procedures.  Include samples of control, construction, and expansion joints in sample panels.  [Mockup] [Field sample] shall be produced by the individual workers who will perform the work for the Project.

      - Accepted [mockup] [field sample] provides visual standard for work of Section.

      - [Mockup] [Field sample] shall remain through completion of the work for use as a quality standard for finished work.

      - Remove [mockup] [field sample] when directed.

  - DELIVERY, STORAGE, AND HANDLING

    - Deliver products in original factory unopened, undamaged packaging bearing identification of product, manufacturer, batch number, and expiration data as applicable.

    - Store the product in a location protected from damage, construction activity, and precipitation in strict accordance with the manufacturer's recommendations.

  - PROJECT CONDITIONS

    - Schedule placement to minimize exposure to wind and hot sun before curing materials are applied.

    - Avoid placing concrete if rain, snow, or frost is forecast within 24-hours.  Protect fresh concrete from moisture and freezing.

    - Comply with professional practices described in ACI 305R and ACI 306R.

  - PRE-JOB CONFERENCE

    - One week prior to placement of concrete, a meeting shall be held to discuss the Project and application methods.

    - It is suggested that the [Architect,] [Landscape Architect,] [Engineer,] General Contractor, [Construction Manager,] Subcontractor, Ready-Mix Concrete Representative, and a Manufacturer's Representative be present.

- PRODUCTS

  - ACCEPT ABLE MANUFACTURER

    - MATCRETE; 1495 Hudson Avenue, Ontario, California 91761, USA. Toll Free: (800) 777-7063.  Tel: (909) 635-0160.  Fax: (909) 635-0165.  Email: info@matcrete.com.
Web: www.matcrete.com.

  - MATERIALS

    - Dry-Shake Colored Hardener: MATCRETE Dustone Color Hardener™; factory proportioned, mixed, and packaged, ready-to-use surface hardener.

    - [Stamping/Imprinting Tools and Materials:]  MATCRETE  Decorative Concrete Stamps™.

    - [Powder Antique Release Agent:]  MATCRETE Dustone Antique Release Agent™. Release agent shall be compatible with stamping/imprinting tools and with dry-shake colored hardener.

    - [UV-Sealer:] MATCRETE Diamond Seal™ Lacquer Sealer. Sealer shall be compatible with powder antique release agent.

  - COLORS [AND PATTERNS]

    - Dry-Shake Color Hardener

      - Color as selected by [Architect] [Landscape Architect] [Engineer] from MATCRETE  Dustone Color Chart.

      - Custom color as selected by [Architect] [Landscape Architect] [Engineer].

    - [Imprinting patterns as selected by [Architect] [Landscape Architect] [Engineer] from MATCRETE  Decorative Concrete Stamps™ Pattern Bulletins.]

    - [Powder Antique Release Agent:] Color as selected by [Architect] [Landscape Architect] [Engineer] from MATCRETE  Dustone Color Chart.

  - CONCRETE MIX DESIGN

    - Minimum Cement Content:  [5] [________] sacks per cubic yard of concrete.

    - Slump of concrete shall be consistent throughout Project at 4-inches or less.  At no time shall slump exceed 5-inches.  [If super plasticizers are allowed, slump shall not exceed 8-inches.]

    - Do not add calcium chloride to mix as it causes mottling and surface discoloration.

    - Supplemental admixtures shall not be used unless approved by manufacturer.

    - Do not add water to the mix in the field.

    - Maximum air content shall not exceed 5 percent.

- EXECUTION

  - CONCRETE PLACEMENT

    - Move concrete into place with square-tipped shovels or concrete rakes.

    - Vibrators, when used, shall be inserted and withdrawn vertically.

    - Concrete shall be struck to specified level with wood or magnesium straight edge or mechanical vibrating screed.

    - The concrete surface shall be further leveled and consolidated with highway magnesium straight edge and/or magnesium bull float.

    - Mechanically float concrete surfaces as soon as concrete surface has taken its initial set and will support weight of a power float machine equipped with float shoes or combination blades and operator.

  - INSTALLATION

    - Apply 2/3 of dry-shake color hardener at specified application rate to freshly floated concrete surface.  Bleed water shall not be present during or following application of first and second shake.

    - Do not throw dry-shake material; distribute evenly by hand.

    - As soon as dry-shake material has absorbed moisture, indicated by uniform darkening of surface, mechanically float concrete surface a second time, just enough to bring moisture from base slab through dry-shake color hardener.

    - Immediately following second floating, apply remaining 1/3 of specified application rate.  If applied by hand, broadcast in opposite direction of first application for a more uniform coverage.  If a mechanical spreader is used, apply the same manner as previously described.

    - As soon as dry-shake material has absorbed moisture, mechanically float concrete surface a third time.

    - Do not add water to the surface.

    - Monitor concrete set time carefully.  When concrete is set adequately to support worker's weight, broadcast powder antique release agent evenly over the slab surface at the rate of approximately 3 to 4 pounds per 100 square feet.

    - Begin imprinting operations immediately after applying powder antique release agent.

    - After the imprinted concrete surface has hardened sufficiently, the remaining unembedded antique release agent should be removed to the degree desired, using high-pressured water, by scrubbing or by buffing.

  - CURING

    - Imprinted concrete should be cured at least 28 days, prior to application of sealer.

    - As soon as possible after antique release has been removed and after moisture content of concrete is low enough that alkali and other salts do not become trapped beneath sealer, normally a minimum of 28 days after placement, apply 2-coats of MATCRETE Diamond Seal™ Lacquer Sealer or specified sealer according to manufacturer’s written instructions. Note that sealers may intensify actual color appearance and make surfaces slightly slippery. When used in areas subject to deicing salts or chemical attack, provide a protective waterproof sealer.

    - There should be no free water on the surface at time of application.

  - PROTECTION OF FINISHED WORK

    - Protect finish work under provisions of Division 1 Section ["Temporary Facilities and Controls."] [________.]

    - Prohibit foot or vehicular traffic on the newly imprinted concrete surface.

    - Barricade area to protect newly imprinted concrete.

    - Protect floor surface from damage until final inspection and acceptance by Owner.

******************************************************************************

Coordinate Schedule name with Drawings or delete Article if Schedule is not required.

******************************************************************************

  - SCHEDULE

    - Refer to Room Finish Schedule for locations of specified floor finish.

- 3.6	APPLICATORS

- A.	For a list of qualified contractors, contact MATCRETE; 1495 Hudson Avenue, Ontario, California 91761, USA. Toll Free: (800) 777-7063.  Tel: (909) 635-0160.  Fax: (909) 635-0165. Email: info@matcrete.com. Web: www.matcrete.com.

- END OF SECTION

© Copyright 2008. All rights reserved.